| Karakaj bb, 75400 Zvornik Republic of Srpska, Bosnia and Herzegovina Phone: +387 (0) 56 / 260 970, 260 435 Fax: +387 (0) 56 / 260 726 http://www.aluminazv.ba | „Alumina” d.o.o. Zvornik |
| --- | --- |

PRODUCT DATA SHEET

CALCINED ALUMINA – METALLURGICAL GRADE

Main application: For aluminium production.

| Chemical Characteristics |
| --- |
| Typical content Guaranteed limits |
| Al2O3 | (%( | 98.8 – 99,0 | 98,7 |
| SiO2 | (%( | 0,005 – 0,010 | 0,015 max |
| Fe2O3 | (%( | 0,008 – 0,012 | 0,018 max |
| Na2Ototal | (%( | 0,30 – 0,35 | 0,42 max |
| CaO | (%( | 0,018 – 0,025 | 0,030 max |
| P2O5 | (%( | 0,0002 – 0,0005 | 0,0009 max |
| TiO2 | (%( | 0,0020 – 0,0027 | 0,003 max |
| ZnO | (%( | 0,017 – 0,020 | 0,022 max |

| Physical Characteristics |
| --- |
| Typical range Guaranteed limits |
| Specific surface area BET | (m2/g( | 75 - 90 | 70 min |
| Bulk Density | (kg/m3( | 1000 - 1050 | 1070 max |
| Loss on ignition L.O.I. (300(C -1000(C) | (%( | 0,6 – 0,9 | 1,00 max |
| Angle of repose | ((( | 32 - 34 | 35 max |
| + 45 μm (wet sieve) | (%( | 88 - 95 | 85 min |
| - 20 μm (wet sieve) | (%( | 1,0 – 2,0 | 2,5 max |

The above values have been determined by the measuring methods and  instruments of  Alumina doo Zvornik.

Product is available in bulk, containers or packaged depending on our customer requirements and available for delivery in the following modes of transport:

- Road - silo trucks, silo containers, pallets

- Rail - bulk and pallets

Compliance: This product is REACH compliant, ask Alumina doo for the associated REACH

registration details.